## Slide 1
Tissue Fabric
Cleaning & Conditioning
Presented by:
John Neun
Engineer
Kadant

## Slide 2
Objectives
Introduction
  What is cleaning & conditioning?
  Theory & practical considerations
Showers
  Fan Jets
  Needle Jets
Felt Dewatering – Uhle Boxes
Applications Specifics
Questions

## Slide 3
Maintain fabric properties over life of fabric – as “steady state” as possible
  remove contaminants
  combat compaction
  preserve permeability
  maintain surface
  retard wear (lubricate)
Why Clean Fabrics?

## Slide 4: Showers
Why Shower?
  Apply chemical
  Apply water
    lubricate
    CLEAN
      flushing
        direct/suction
        flooded nip
      kinetic energy
Shower Types
  -Fan Jet
  even distribution
  -Needle Jet
  apply energy
  -Single Jet Scanning
Tappi TIP 0404-61, “Paper Machine Shower Recommendations”

## Slide 5: Fan Shower Profile Management

## Slide 6: Fan Nozzle Variation:
• Flow Distribution
• Total Flow Volume

## Slide 7: Nozzle Flow Distribution Tester

## Slide 8: Nozzle Spray Distribution
40 - 45 degrees
.047 - .054 inch orifice
pattern width
%-flow
0
12

## Slide 9: Total Flow Variations Nozzles of the Same Type
Standard Deviation/Average Flow
Nozzle
Type 1
Type 2
Type 3
25 - 30
2%
4%
2%
o
o
30 - 35
6%
3%
o
o
40 - 45
8%
3%
3%
o
o
55 - 60
4%
3%
o
o
Flow does not vary very much from nozzle to nozzle

## Slide 10: Nozzle Spray Pattern Distribution
minimum
average
maximum
"uncertainty
zones"

## Slide 11: Nozzle Spacing
wet streak
dry streak
wet streak
almost inevitable
Spaced for average pattern width
  50% chance of dry streak
  50% chance of wet streak
Spaced for minimum width
  Probable wet streak
  No dry streaks

## Slide 12: Overlapped Nozzles:
•Conservative Approach
•Precludes Dry Streaks
•Causes Wet Streaks

## Slide 13: Typical Single Coverage Fan Shower Arrangement
1x coverage: each nozzle covers the same CD width
Pattern edges overlap to prevent dry streaks

## Slide 14: Shower Layout
overlap areas:
double coverage
single coverage
areas
overlap areas:
triple coverage
double
coverage
areas
Single coverage is a must
Multiple coverage is better
  Attenuates variation (3:2 is better than 2:1)
  “insurance” against plugged nozzles

## Slide 15: Machine Width Shower Distribution
0
0.04
0.08
0.12
0.16
gpm/in.
300 inches wide
45 degree nozzles
6 inch centers
1/2 inch pattern overlap
0
0.04
0.08
0.12
0.16
12-inch oscillator stroke
 | Not Oscillated | Oscillated
Avg. flow (gpm/inch) | .079 | .079
Standard Deviation | .019 (24%) | .003 (4%)

## Slide 16: Flooded Nip Shower
Full width flooded nip shower
  Provides outstanding Knock-off & cleaning performance
Excellent tool for cleaning inside surface &
powering out voids with modest water volume
  Helps debris off fabric, provides flushing water to clean fabric
  Pointed just before nip, FORMS PUDDLE
  Puddle insures even distribution, not nozzle-shower
  configuration
  Allows roll’s fluid mechanics to force contaminates out
If it’s the only full width fan shower, consider the applied energy
  Operation below RVV yields far less driving force for knock-off
  RVV is VERY water intensive (high volume)
  Optimum cleaning occurs at RVV, BUT good cleaning can be achieved at lower volumes
NOTE: the above is for flooded nip wire showers. For felt flooded nips, volume to achieve void volume (gpm) is
Fabric Width(in) x Fabric Wt.(oz/ft2) x Speed(fpm) x C – all other shower flows
Where C = 0.000063
12”- 15”
(300 – 380 mm)

## Slide 17: Running Void Volume
R.V.V. (gpm)= CxWxSxVxSF
19.25
EXAMPLE flooded nip
1550 fpm-Speed factor = 1.3
Full coverage flow =
340 gpm on new wire
Re- calculate
Both S and SF for other
Machine speeds.
Note that void volume and
Speed factor are
Dimensionless.
C= Caliper of Fabric in Inches
W= Fabric Width in Inches
S= Speed in FPM
V= Void Volume (use 0.6)
SF= Speed Factor for wires

## Slide 18: Flooded Nip Showers
Flooded nip placement: note landing on roll before nip to form puddle
Tissue felt flooded nip
FNKO running at full (knock-off) volume
Flooded nip running at reduced volume sufficient for cleaning

## Slide 19: Needle Jet Showers

## Slide 20: How Do Needle Showers Work?
1.Pressure,Force?
pressure
area
3. Impulse?
mass
velocity
2. Energy, Momentum?
velocity
mass
time

## Slide 21: “Why’s” of Needle Jets
Cleaning depends on distance from the fabric
Cleaning is proportional to energy Cleaning = f(energy/time) = f(power)
3.
Energy
=
1
2
mv
2
v
µ
p
m
µ
a
µ
d
2
shower effectiveness

## Slide 22: Inside HPS for through cleaning
Laminar flow penetrates better, jet distance < 4” for through cleaning

## Slide 23: Sheet Side HPS for surface cleaning
Maximize surface cleaning effectiveness/pressure > 6 in.
shower effectiveness

## Slide 24: How Important is Dispersal Area?
.014 dia. nozzle
2,300 psi
4,700 rpm
.014 dia. nozzle
2,300 psi
0 rpm

## Slide 25: Power Application: Jet Vs. Fan
Typical Nozzle: .040 diameter, 150 psi
.040 Jet | .040 600 fan MD | .040 600 fan CD
.36 gpm | .46 gpm | .46 gpm
14 watts | 19 watts | 19 watts
11,000 watts/in2 | 78 watts/in2 | 78 watts/in2
 |  | 467 watts/in2 effective

## Slide 26: Felt HPN Jet Quality
Jet Quality, significant impact on cleaning performance
“Glass Rod” type
of appearance
GOOD
Energy is disbursed
over an area 6X greater
POOR

## Slide 27: How Far From the Fabric?
Distance from Orifice
Relative
Cleaning
Action
(measured with
piezocrystal
sensor)

## Slide 28: Best Jet Angle
Vector logic for “chasing” wire for INSIDE
Vector logic for “chiseling” wire for OUTSIDE
Fabric speed
Shower stream
Resultant vector (from contaminant frame of reference) into fabric depending on speed match
“through cleaning”
Fabric speed
Shower stream
Resultant vectors apply energy to surface contaminants, and use some energy to get contaminants OFF fabric
“surface cleaning”

## Slide 29: Application to Fabric Conditioning
For sheet side cleaning
  Use region of peak dynamic power
  Peak power occurs anywhere from 6 to 10 inches
  Oscillation for even effect
For inside cleaning
  Use region of optimum penetration
  Laminar flow penetrates better than 2 phase flow
  Shower should be close to fabric (3-4 in.)
Replace nozzles regularly to maintain good patterns

## Slide 30: On Roll or In Space?
Energy transfer
  If wire cannot recoil on impact energy transfer is optimized  target shower on roll
Mist control
  If roll is behind wire, there is no through flow  no inside fabric run mess  target shower on roll
Chisel or following angle?
  Chisel is optimum for contaminant impact
  Mist control is probably more important  point shower in direction for best mist control

## Slide 31: What About Felt Seams?
Clean vs. destroy
Seam needs to be continuous with felt
“Chiseling” angle tends to push seam batt out of seam
Following angle tends to lift seam flap
Ideal: resultant angle perpendicular, keep material in seam
Best angle for seam: slight following angle with resultant perpendicular to felt
New Condition
Peel Back
Flap wornout/damaged
Energy Vector
Fabric speed
Shower stream
Resultant energy vector

## Slide 32: Oscillation of High Pressure Showers
It’s not just a good idea,
It’s the law!

## Slide 33: Crank Arm Oscillators

## Slide 34: Importance of Proper Oscillation

## Slide 35: Low Speed Oscillation
Coordinate oscillator speed with fabric speed
Perfect, even coverage

## Slide 36: Even, Uniform Coverage
Oscillator Speed Calculations
Traversing Speed = M/C speed x Noz. Dia.
Fabric Length

## Slide 37: A Note on Scanning Jet Showers
Continuous cleaning: STEADY STATE
Treat Streaks
  direct cleaning to area of greatest concern
  maintain better profiles
Reliability
  Shower beam
  High pressure supply system
  Maintenance program

## Slide 38: Other Profile Considerations
The Battle Against
Nozzle Plugging

## Slide 39: Filtration vs. Nozzle Plugging

## Slide 40: Brush Showers

## Slide 41: Filter media specification
Nozzle orifice size defines the barrier dimension
Loading defines the frequency of service
  The filter’s total open area determines the ΔP

## Slide 42: Felt Dewatering
Uhle boxes
  Remove water from the felt
  Help keep felts clean
Vacuum is applied to felts via stationary boxes to remove water from them
  Called uhle boxes or suction boxes
  Vacuum levels are conventionally up to 15 inHg, but can be as high as 20+ inHg (highly loaded presses, heavy felts)
  New, more permeable felts have lower vacuums
Conventionally, presses express water from the sheet to the felt, and water is then removed from the felt at the uhle box
  Many modern machines depend on press nip dewatering; water is removed from the felt at the press making uhle dewatering less critical

## Slide 43: Traditional Uhle Sizing
Calculate dwell time for machine conditions, target moisture content.
  First press: .8 - .7 lb H2O/lb felt
  Second press: .7 - .62 lb H2O/lb felt
  Third press: .6 - .54 lb H2O/lb felt
  F2 = 1.23 • F1^(.819) • Q^(-.024) • dP^(-.124) • D^(-.096)
  NOTE: this equation was determined empirically and felts have changed radically. It can be used only for rough estimates of dewatering
Calculate airflows with Decrosta equation. (still gives a reasonable estimate of airflow)

## Slide 44: Decrosta Airflow Equation
V =
m
.628
p1
.069 x DP x t x perm
.476
.11
.916
d
V =
m
p1
DP t perm
d
Just like

## Slide 45: Dwell Time
=
5 x no. of slots x slot width (inches)
speed (fpm)
dwell time (seconds)

## Slide 46: Pipe Sizing
Air Velocity limit: pressure drop across pipe is less than 2 in.- H2O
  <3000 fpm before separator
  <5000 fpm after separator
  <500 fpm in separator
Structure: maximum stress below 16,000 psi

## Slide 47: Slot Width
Dwell time is the ONLY effect of slot width:
  1 x 1” = 2 x 1/2” FOR DEWATERING
More narrow slots are better than fewer wide slots: felt wear
Fewer wider slots are less likely to plug
“Break to atmosphere” between slots doesn’t matter.

## Slide 48: Wear Surface Materials
Cost Vs. Benefit:
cover life
fabric life

## Slide 49: Slot Width, Fabric Penetration
Wide Slots
  Provide high dwell time
  Create high fabric wear
  Create high seam stresses
¾ vs 1.5 inch slot width, 15 in-Hg
  Fabric deflection: .035 vs .138 in.
  Edge angle: 100 vs 200
  At least twice the damage
Multiple narrower slots are better
  Less fabric wear
  Less seam wear
Slots that are too narrow can plug
  About 3/8 inch width is a good practical lower limit
tension
tension
vacuum
Chart: Slot Width (in.)
| 0 | 0.25 | 0.27500000000000002 | 0.30000000000000032 | 0.32500000000000634 | 0.35000000000000031 | 0.37500000000000488 | 0.4 | 0.42500000000000032 | 0.45 | 0.47500000000000031 | 0.5 | 0.52500000000000002 | 0.55000000000000004 | 0.57500000000000062 | 0.60000000000000064 | 0.62500000000001132 | 0.65000000000001279 | 0.67500000000001448 | 0.70000000000000062 | 0.72500000000000064 | 0.75000000000001132 | 0.77500000000001001 | 0.8 | 0.82500000000000062 | 0.85000000000000064 | 0.87500000000001132 | 0.9 | 0.92500000000000004 | 0.95000000000000062 | 0.97500000000000064 | 1 | 1.0249999999999753 | 1.0499999999999683 | 1.0749999999999778 | 1.0999999999999719 | 1.1249999999999996 | 1.1499999999999748 | 1.1749999999999994 | 1.1999999999999778 | 1.2249999999999714 | 1.2499999999999618 | 1.2749999999999744 | 1.2999999999999672 | 1.3249999999999778 | 1.349999999999971 | 1.3749999999999978 | 1.3999999999999739 | 1.424999999999967 | 1.4499999999999558 | 1.4749999999999708 | 1.4999999999999614
20 inHg | 0 | 0.0021929 | 0.0026534 | 0.0031577 | 0.0037059 | 0.004298 | 0.0049339 | 0.0056137 | 0.0063374 | 0.0071049 | 0.0079162 | 0.0087714 | 0.0096705 | 0.010613 | 0.0116 | 0.012631 | 0.013705 | 0.014824 | 0.015986 | 0.017192 | 0.018442 | 0.019736 | 0.021073 | 0.022455 | 0.02388 | 0.025349 | 0.026862 | 0.028419 | 0.03002 | 0.031665 | 0.033353 | 0.035086 | 0.036862 | 0.038682 | 0.040546 | 0.042454 | 0.044405 | 0.046401 | 0.04844 | 0.050523 | 0.05265 | 0.054821 | 0.057036 | 0.059295 | 0.061597 | 0.063944 | 0.066334 | 0.068768 | 0.071246 | 0.073768 | 0.076333 | 0.078943
15 inHg | 0 | 0.0016446 | 0.00199 | 0.0023683 | 0.0027794 | 0.0032235 | 0.0037004 | 0.0042103 | 0.004753 | 0.0053286 | 0.0059372 | 0.0065786 | 0.0072529 | 0.0079601 | 0.0087002 | 0.0094731 | 0.010279 | 0.011118 | 0.011989 | 0.012894 | 0.013831 | 0.014802 | 0.015805 | 0.016841 | 0.01791 | 0.019012 | 0.020147 | 0.021315 | 0.022515 | 0.023749 | 0.025015 | 0.026314 | 0.027646 | 0.029011 | 0.030409 | 0.03184 | 0.033304 | 0.034801 | 0.03633 | 0.037893 | 0.039488 | 0.041116 | 0.042777 | 0.044471 | 0.046198 | 0.047958 | 0.04975 | 0.051576 | 0.053434 | 0.055326 | 0.05725 | 0.059207
10 inHg | 0 | 0.0010964 | 0.0013267 | 0.0015789 | 0.001853 | 0.002149 | 0.002467 | 0.0028069 | 0.0031687 | 0.0035524 | 0.0039581 | 0.0043857 | 0.0048353 | 0.0053067 | 0.0058001 | 0.0063154 | 0.0068527 | 0.0074119 | 0.007993 | 0.008596 | 0.009221 | 0.0098679 | 0.010537 | 0.011227 | 0.01194 | 0.012675 | 0.013431 | 0.01421 | 0.01501 | 0.015832 | 0.016677 | 0.017543 | 0.018431 | 0.019341 | 0.020273 | 0.021227 | 0.022203 | 0.0232 | 0.02422 | 0.025262 | 0.026325 | 0.027411 | 0.028518 | 0.029647 | 0.030799 | 0.031972 | 0.033167 | 0.034384 | 0.035623 | 0.036884 | 0.038167 | 0.039471
5 inHg | 0 | 0.00054821 | 0.00066334 | 0.00078943 | 0.00092648 | 0.0010745 | 0.0012335 | 0.0014034 | 0.0015843 | 0.0017762 | 0.0019791 | 0.0021929 | 0.0024176 | 0.0026534 | 0.0029001 | 0.0031577 | 0.0034263 | 0.0037059 | 0.0039965 | 0.004298 | 0.0046105 | 0.0049339 | 0.0052683 | 0.0056137 | 0.0059701 | 0.0063374 | 0.0067156 | 0.0071049 | 0.0075051 | 0.0079162 | 0.0083383 | 0.0087714 | 0.0092155 | 0.0096705 | 0.010136 | 0.010613 | 0.011101 | 0.0116 | 0.01211 | 0.012631 | 0.013163 | 0.013705 | 0.014259 | 0.014824 | 0.015399 | 0.015986 | 0.016583 | 0.017192 | 0.017811 | 0.018442 | 0.019083 | 0.019736
Chart: Slot Width (in.)
| 0 | 0.25 | 0.27500000000000002 | 0.30000000000000032 | 0.32500000000000634 | 0.35000000000000031 | 0.37500000000000488 | 0.4 | 0.42500000000000032 | 0.45 | 0.47500000000000031 | 0.5 | 0.52500000000000002 | 0.55000000000000004 | 0.57500000000000062 | 0.60000000000000064 | 0.62500000000001132 | 0.65000000000001279 | 0.67500000000001448 | 0.70000000000000062 | 0.72500000000000064 | 0.75000000000001132 | 0.77500000000001279 | 0.8 | 0.82500000000000062 | 0.85000000000000064 | 0.87500000000001132 | 0.9 | 0.92500000000000004 | 0.95000000000000062 | 0.97500000000000064 | 1 | 1.0249999999999753 | 1.0499999999999683 | 1.0749999999999778 | 1.0999999999999719 | 1.1249999999999996 | 1.1499999999999748 | 1.1749999999999994 | 1.1999999999999778 | 1.2249999999999714 | 1.2499999999999618 | 1.2749999999999744 | 1.2999999999999672 | 1.3249999999999778 | 1.349999999999971 | 1.3749999999999978 | 1.3999999999999739 | 1.424999999999967 | 1.4499999999999558 | 1.4749999999999708 | 1.4999999999999614
20 inHg | 0 | 2.0094 | 2.2102 | 2.4109 | 2.6115 | 2.8121 | 3.0126 | 3.213 | 3.4134 | 3.6137 | 3.8139 | 4.0139 | 4.2139 | 4.4138 | 4.6136 | 4.8133 | 5.0128 | 5.2123 | 5.4116 | 5.6107 | 5.8098 | 6.0087 | 6.2074 | 6.406 | 6.6045 | 6.8027 | 7.0009 | 7.1988 | 7.3966 | 7.5942 | 7.7916 | 7.9889 | 8.1859 | 8.3828 | 8.5794 | 8.7759 | 8.9721 | 9.1682 | 9.364 | 9.5596 | 9.7549 | 9.9501 | 10.145 | 10.3396 | 10.5341 | 10.7283 | 10.9222 | 11.1159 | 11.3093 | 11.5025 | 11.6954 | 11.888
15 inHg | 0 | 1.5073 | 1.658 | 1.8086 | 1.9592 | 2.1098 | 2.2604 | 2.4109 | 2.5614 | 2.7118 | 2.8622 | 3.0126 | 3.1629 | 3.3132 | 3.4635 | 3.6137 | 3.7638 | 3.9139 | 4.064 | 4.2139 | 4.3639 | 4.5137 | 4.6635 | 4.8133 | 4.963 | 5.1126 | 5.2621 | 5.4116 | 5.561 | 5.7103 | 5.8595 | 6.0087 | 6.1577 | 6.3067 | 6.4556 | 6.6045 | 6.7532 | 6.9018 | 7.0504 | 7.1988 | 7.3472 | 7.4954 | 7.6436 | 7.7916 | 7.9396 | 8.0874 | 8.2352 | 8.3828 | 8.5303 | 8.6777 | 8.825 | 8.9721
10 inHg | 0 | 1.005 | 1.1055 | 1.206 | 1.3064 | 1.4069 | 1.5073 | 1.6078 | 1.7082 | 1.8086 | 1.909 | 2.0094 | 2.1098 | 2.2102 | 2.3105 | 2.4109 | 2.5112 | 2.6115 | 2.7118 | 2.8121 | 2.9124 | 3.0126 | 3.1128 | 3.213 | 3.3132 | 3.4134 | 3.5135 | 3.6137 | 3.7138 | 3.8139 | 3.9139 | 4.0139 | 4.114 | 4.2139 | 4.3139 | 4.4138 | 4.5137 | 4.6136 | 4.7135 | 4.8133 | 4.9131 | 5.0128 | 5.1126 | 5.2123 | 5.3119 | 5.4116 | 5.5112 | 5.6107 | 5.7103 | 5.8098 | 5.9092 | 6.0087
5 inHg | 0 | 0.50255 | 0.55281 | 0.60306 | 0.65331 | 0.70356 | 0.75381 | 0.80405 | 0.8543 | 0.90454 | 0.95479 | 1.005 | 1.0553 | 1.1055 | 1.1557 | 1.206 | 1.2562 | 1.3064 | 1.3567 | 1.4069 | 1.4571 | 1.5073 | 1.5576 | 1.6078 | 1.658 | 1.7082 | 1.7584 | 1.8086 | 1.8588 | 1.909 | 1.9592 | 2.0094 | 2.0596 | 2.1098 | 2.16 | 2.2102 | 2.2604 | 2.3105 | 2.3607 | 2.4109 | 2.4611 | 2.5112 | 2.5614 | 2.6115 | 2.6617 | 2.7118 | 2.762 | 2.8121 | 2.8622 | 2.9124 | 2.9625 | 3.0126
Catenary Deflection

## Slide 50: Seamed Fabrics
Herringbone Design
Zig Zag Design
Trapezoid Design
Dwell time determines dewatering
Make sure dwell time is even across width of fabric

## Slide 51: Streaks from Herringbone Covers
Worn covers are “re-injecting” water back into felt at the trailing edge of each slot

## Slide 52: Herringbone Covers (continued)
Worn covers
  water is re-injected into the felt where the inside trailing edge has been worn away

## Slide 53: Reading streaks
Press fabric streaks (a mixed bag)
  Narrow streaks every 2” – 3”……Herringbone cover geometry or worn
  Narrow streaks every 6”…...……OPN oscillator reversal dwell
  Dark 6” bands…………………….Single plugged or poor nozzle
  Very Dark 6” band………………..Adjacent nozzles plugged or poor
  Bands after chemical wash……..Shower with plugged nozzles
  Uneven batch shows up as diminished even color change across felt
  Example of felt streaks (with typical 6” nozzle spacing & 12” oscillator)

## Slide 54: Strategy for Ideal Cleaning Applications

## Slide 55: Wire Cleaning Strategy
Create constant fluid motion to the sheet side then, utilizing outside rolls with doctors and showers to flush wire.
Inside rolls & catch pans for stapled fibers

## Slide 56: Felt Cleaning Applications
Face side Needle Jet Shower must be setup for Surface cleaning
Uhle box removes loosened surface and interstitial debris
Face side roll with Doctor removes surface contaminates
Create constant migration of contaminates to face side
  Inside Needle Jet
  Inside Chemical
  Nip Shower
  Finally – the Uhle Box

## Slide 57: Contaminants and Conditioning
What’s the problem?
Permeability, surface, fabric life?
Fabric type
Particulate or “gel?”
Determines:
WATER CONTENT, VOLUME
Shower location and type,
flow, angle
Vacuum requirements

## Slide 58: Crescent Former Machine
SPR

## Slide 59: Forming Section (Crescent Former)
3
6
1
5
4
2
9
9
9
9
9
9

## Slide 60: Press Section (Crescent Former)
SPR
B
Alt
E
E
E
D
D
A
C
YB

## Slide 61: Suction Pick-up
B
A
C
F
Alt.
D
D
E
E
E
YB

## Slide 62: Suction Breast Roll
3
1
7
9
9
6
4
2
5
10
8

## Slide 63: S-Wrap
3
1
1
2
6
6
3
9
9
9
9
9
9
4
4
2
9
9
10
10

## Slide 64: C Wrap
3
1
1
6
6
3
9
9
9
9
9
9
2
7
2
10
10
4
4

## Slide 65: Some Relevant TAPPI TIPs
0404-27, Press Fabric Dewatering and Conditioning – Suction Box (Uhle Box) Design and Vacuum Requirements
0404-51, Paper Machine Clothing Cleaning and Conditioning for Recycled Fiber Use
0404-52, Press Section Optimization
0404-57, Troubleshooting Cross-Machine Direction Moisture Profile Problems
0404-61, Paper Machine Shower Recommendations
0404-67, Paper Machine Doctor Recommendations
0502-22, Paper Machine Water Efficiency

## Slide 66: Summary
Fan Showers – Even Distribution
  Overlap nozzles, consider oscillating critical showers
  Double or triple coverage nozzle spacing is best
  Flooded Nip
    Running Void Volume for knock off
    Some volume less than RVV for some cleaning
    For felts: RVV – other shower volume
Needle Jets – Power Application
  Use 6 inch stand-off on sheet side, 4 inches or less on inside
  Use pressure as low as possible (400 psi max forming, 250 psi max felts)
  Oscillate evenly @ twice nozzle spacing, 1 noz. diameter/fabric revolution
  ”Chisel” angle, 150 into fabric on sheet side showers
  Perpendicular or 150 chasing angle for inside showers
Change nozzles to maintain good patterns (rule of thumb, once/year)
Basic fabric cleaning strategy: move contaminants out of fabric (flush), and then off (needle jets, wash rolls) in direction from which they came
Uhle Boxes – Dewater and clean felts
  Between 2 – 4 ms dwell
  15 inHg (or a little more) for broken-in felts

## Slide 67
Thank you
John Neun
john.neun@gmail.com