## Slide 1: Factors Affecting Phosphorus Uptake/Dissolution in Slaking/Causticizing
Gateway to
the Future
Maryam Mousavi
Supervisor:
Prof. Nikolai DeMartini
University of Toronto

## Slide 2: About Phosphorus
2
P can enter the mill with wood, biosludge and biofuels
Phosphorus is known to decrease lime availability
The main purge points are lime mud and lime kiln dust

## Slide 3: Why phosphorus is important ?
P compounds
Formation of non-reactive Ca-PO4
Lime availability
P decreases lime availability
Deadload in lime mud
Increased energy and lime consumption
Biofuels
  Introduction of P with biofuels

## Slide 4: Background
Previous work showed the form of P in lime and lime mud is rhenanite (NaCaP)
There is a competition between PO43- and CO32- for calcium during slaking and causticizing

## Slide 5: Objectives
To understand factors affecting P uptake during slaking and causticizing:
Effect of ionic strength :
Change TTA (constant sulfidity)
Change sulfidity (constant TTA)
Effect of P concentration :
Change the PO43- concentration in green liquor
Effect of liming ratio
Comparison between the behavior of reburned lime and technical-grade CaO

## Slide 6: Recausticizing Process
Lime
Courtesy of Valmet
Lime Availability :
  The amount of CaO available for slaking

## Slide 7: Experimental Set-up
Experimental Set-up
Stirrer Control
Teflon Bottle
Thermometer
95
Temperature Control
Stir Bar
For all experiments, synthetic green liquor was made with Na2CO3 and Na2S

## Slide 8: Experimental : Effect of Ionic Strength
Variable | 
TTA | 96-140 g/L Na2O
Sulfidity | 10—30 % (TTA basis)
P concentration | 50 mg/L as Na3PO4
Liming ratio | 1 0.1
Slaking and causticizing time | 4 h
Lime type | Technical-grade CaO and reburnt lime
Variable | 
TTA | 96-140 g/L Na2O
Sulfidity | 10—30 % (TTA basis)
P concentration | 50 mg/L as Na3PO4
Liming ratio | 
Slaking and causticizing time | 4 h
Lime type | Technical-grade CaO and reburnt lime

## Slide 9: Effect of Ionic Strength
Chart: Ionic Strength (mol/L)
| 4.71 | 5.15 | 5.58 | 6.01 | 5.72 | 5.58 | 5.44 | 5.3 | 5.71 | 6.66 | 6.66 | 6.6
Reburned Lime | 3.65 | 4.35 | 3.25 | 7.95 | 4.5 | 3.2 | 3.6 | 4.5 | 7.5 | 12.5 | 10.5 | 11
Technical-grade CaO | 9.8 | 20.5 | 21.3 | 20.5 | 23.5 | 19 | 23
P concentration in WL remains constant up to an ionic strength of 5.6 M. But increases linearly beyond this point.

## Slide 10: Effect of CO3 on the Final P Concentration in WL
Chart: g CO3/L
| 80 | 87 | 94 | 102 | 101 | 95 | 88 | 82 | 87 | 102 | 95 | 102
Reburned Lime | 3.65 | 4.35 | 3.25 | 7.95 | 4.5 | 3.2 | 3.6 | 4.5 | 7.5 | 12.5 | 10.5 | 11
Technical-grade CaO | 9.8 | 20.5 | 21.3 | 20.5 | 23.5 | 19 | 23
There was no clear correlation between the final phosphate concentration in the white liquor and carbonate concentration
The P concentration at all ionic strengths was higher for Tech-grade CaO than for the reburned lime. Likely due to a difference in their reactivity

## Slide 11: Experimental : Changing Green Liquor P Concentration
Variable | 
TTA | 111 g/L Na2O
Sulfidity | 14 % (TTA basis)
P concentration | 25, 50 and 75 mg/L as Na3PO4
Liming ratio | 1 0.1
Slaking and causticizing time | 4 h
Lime type | Technical-grade CaO and reburnt lime
Variable | 
TTA | 111 g/L Na2O
Sulfidity | 14 % (TTA basis)
P concentration | 25, 50 and 75 mg/L as Na3PO4
Liming ratio | 
Slaking and causticizing time | 4 h
Lime type | Technical-grade CaO and reburnt lime

## Slide 12: Effect of P Concentration on P Pick-up/Dissolution (Reburnt Lime)
Chart: Time (min)
| 0 | 5 | 10 | 15 | 30 | 60 | 120 | 240
P=25 ppm | 27.2 | 49 | 36.35 | 30.05 | 23.15 | 14.3 | 8.95 | 8.15
P=50 ppm | 53.2 | 18.68 | 10.92 | 9.48 | 5.94 | 3.88 | 3.52 | 3.4 | 3.16
P=75 ppm | 78.13 | 60.8 | 34.7 | 25.65 | 15.6 | 11.99 | 8.29 | 7.59
Error bars represent 1 standard deviation of at least 5 replicate analyses of the samples.

## Slide 13: Effect of P Concentration on P Pick-up/Dissolution (Technical-Grade CaO)
Chart: Time (min)
| 0 | 5 | 10 | 15 | 30 | 60 | 120 | 240
P=25 ppm | 23.58 | 7.08 | 7.1 | 6.66 | 8.32 | 8.2
P=50 ppm | 47.03 | 14.3 | 11.1 | 10.85 | 12.1 | 15.9
Error bars represent 1 standard deviation of at least 5 replicate analyses of the samples.

## Slide 14: Proposed Dissolution Mechanism
Ca(OH)2(s) + CO32-(aq) CaCO3(s) + 2OH-(aq)
Ca(OH)2 (s) + Na+(aq) + PO43-(aq) NaCaPO4(s) + 2OH-
NaCaPO4(s) + CO32-(aq)⇌ CaCO3(s) + Na+(aq) + PO43- (aq)

## Slide 15
Separate Slaking and Causticizing Experiment
Reburnt lime was first slaked in water and then the slaked lime was added to Green liquor.
Variable | 
TTA | 111 g/L Na2O
Sulfidity | 14 % (TTA basis)
P concentration | 25 mg/L as Na3PO4
Liming ratio | 1 0.1
Slaking and causticizing time | 4 h
Lime type | reburnt lime
Variable | 
TTA | 111 g/L Na2O
Sulfidity | 14 % (TTA basis)
P concentration | 25 mg/L as Na3PO4
Liming ratio | 
Slaking and causticizing time | 4 h
Lime type | reburnt lime

## Slide 16: Results : Separate Slaking and Causticizing Experiment
Chart: Time(min)
| 0 | 5 | 10 | 15 | 30 | 60 | 120 | 240
TTA130S25P25 | 1 | 0.096324 | 0.069118 | 0.080882 | 0 | 0 | 0 | 0
Samples were taken after the pre-slaked lime was added to the green liquor
Phosphate reacts with Ca(OH)2, resulting in the formation of rhenanite
The rate of slaking is likely the primary factor influencing the rate of (P) uptake

## Slide 17
Experimental :Effect of Liming Ratio
Variable | 
TTA | 111 g/L Na2O
Sulfidity | 14 % (TTA basis)
P concentration | 50 mg/L as Na3PO4
Liming ratio | 0.5 , 0.75 , 1 and 1.5
Slaking and causticizing time | 4 h
Lime type | Technical-grade CaO and reburnt lime

## Slide 18: Effect of Liming Ratio : Reburnt Lime
Chart: Time (min)
| 0 | 5 | 10 | 15 | 30 | 60 | 120 | 240
Liming ratio=0.5 | 52.6 | 58 | 72.4 | 73.2 | 74.86 | 77.5 | 79.1 | 82.5
Liming ratio=0.75 | 52.6 | 48.9 | 60.84 | 59.52 | 53.16 | 48.1272 | 38.46 | 29.1
Liming ratio= 1 | 52.6 | 18.65 | 10.4 | 6.2 | 4.11 | 3.8 | 3.8 | 3.37
Liming ratio=1.5 | 52.6 | 10.38 | 8.44 | 8 | 6.6 | 6.4 | 5.28 | 4.84

## Slide 19: Effect of Liming Ratio : Technical-Grade CaO
Chart: Time(min)
| 0 | 5 | 10 | 15 | 30 | 60 | 120 | 240
Liming ratio= 0.5 | 52.6 | 28.8 | 30.2 | 31.6 | 34.6 | 35.6 | 37.2 | 40
Liming ratio = 0.75 | 52.6 | 22.76 | 22 | 23.4 | 24.48 | 26.2946 | 29.28 | 31.1
Liming ratio=1 | 52.6 | 14.3 | 11.1 | 10.85 | 12.1 | 15.9 | 16.1 | 16.95

## Slide 20: Conclusions
P in the reburnt lime can be partially soluble in water during slaking
For reburned lime, ionic strength can impact uptake of P by lime above an ionic strength of 5.6 M
The carbonate concentration does not have a clear impact beyond impacting ionic strength.
P pick-up seems to mostly occur during causticizing
-> Ca(OH)2 seems to be the active solid
Reaction for dissolution of rhenanite has been proposed
P pick-up from the green liquor increases by increasing the liming ratio

## Slide 21
Thank You